## Slide 1: 角膜氧供与接触镜配戴
A6
2016-June-20

## Slide 2: Attributions
Lecture contributors* | Robert Terry, Lewis Williams
Lecture editor** | Percy Lazon
IACLE executive editor** | Lakshmi Shinde
IACLE reviewer** | Nilesh Thite, Lewis Williams
Lecture updated | 2015 Nov
Lecture content rechecked | 2016 June
* Original author(s) of lecture(s) | **2015 Editors and reviewers

## Slide 3: 编审者
撰稿人* | Robert Terry, Lewis Williams
编辑** | Percy Lazon
IACLE 责任编辑** | Lakshmi Shinde
IACLE 审稿人** | Nilesh Thite, Lewis Williams
更新时间 | 2015 年11月
内容复审时间 | 2016 年6月
* 原作者 | **2015 编辑和审稿人

## Slide 4: 通过教育基金和实物捐赠，IACLE开发和提供隐形眼镜教育
CIBA Vision Bausch & Lomb
Allergan
AMO
Ocular Sciences
Wesley Jessen
Menicon
Paragon
Pilkington Barnes-Hind
Aspect Vision Care
铂金赞助商
白银赞助商
捐赠资助

## Slide 5
国际接触镜教育者学会是IACLE接触镜镜课程（简称ICLC）所有格式和版本的唯一所有者，受版权保护。若要获得该接触镜材料，您需要同意以下条款：
IACLE接触镜课程只能用于个人或学习用途。未经IACLE书面同意，严禁传播或销售ICLC的全部或部分内容，或将本教材用于教育及个人以外的用途。除以下声明外，不得复制、重新发布、出版或分发ICLC中包含的任何材料。
你可以在个人或教育使用时打印课程材料。所有版权信息，包括IACLE徽标必须保留在材料上。使用ICLC的任何内容，包括文本，图片或注释等必须提供合适的引用标记。
版权声明

## Slide 6: 出版 国际接触镜教育者学会(IACLE) 2016修订版 © 国际接触镜教育者学会2000-2015 版权所有。未经国际接触镜教育者学会事先书面许可，本出版物的任何部分不得复制、储存在检索系统中，或以任何形式或传播： 国际接触镜教育者学会 IACLE秘书处， PO Box 656 KENSINGTON NSW 2033 Australia 电子邮件：iacle@iacle.org

## Slide 7
氧气
20.95%
其他
0.97%
氮气
78.09%
角膜氧供来源: 干燥大气
Notes: 12
12
Measurement of Corneal O2 Requirements
Any ↓ in the amount of O2 available to a metabolically active tissue can significantly alter the physiological equilibrium of the component cells & therefore, the tissue itself. The cornea is no exception.
An adequate supply of O2 to the cornea is vital to its metabolic processes & the maintenance of its structural integrity. For successful CL wear, the CLs fitted must supply at least the minimum level of O2 the cornea requires. While it would be useful to know the minimum O2 requirement of the individual cornea, this is usually not practical in routine CL practice. Instead, a CL is selected which should allow a level of O2 above, & preferably well above, the ‘average’ minimum required.
A considerable amount of research has been undertaken to determine the critical O2 needs of the cornea. While there are some differences in the conclusions of such research, there is general agreement on the O2 levels required for safe daily & overnight wear of CLs. Until recently, many of the CLs marketed were incapable of meeting the relatively high levels of O2 that much of the published research indicated was required, especially in relation to overnight extended wear. Products are now becoming available which exceed the recommendations for this mode of wear by a comfortable margin.
Gaseous Components of the Atmosphere
A substantial but minor part of the earth’s atmosphere is made up of gaseous O2, which is the ‘fuel’ for many of the metabolic functions within the body. O2 makes up approximately 21% of the earth’s atmosphere.
CO2 levels have now reached 400 ppm (0.04%) a level it is expected to maintain or exceed for years to come.

## Slide 8
其他气体
二氧化碳
氩气
氖气
角膜氧供来源: 大气 (其他)
Notes: 12
12
Other constituents of potential relevance to CL wear and/or the cornea are carbon dioxide (CO2) & water vapour. However, in the normal atmosphere, the CO2 levels are so low as to be practically insignificant & the amount of water vapour present is very variable & will be dealt with separately (see later).

## Slide 9
–10
0
10
20
30
40
50
100
0
20
40
60
80
水蒸气压力(mm Hg)
温度 (°C)
水蒸气压力vs 温度
Notes: Partial Pressure (Tension) of O2
In percentage terms, the components of the atmosphere do not vary with altitude. However, the pressure of the atmosphere on the body (atmospheric pressure or barometric pressure) ↓ significantly with altitude.
There is also an attendant ↓ in the partial pressure of O2. However, as a percentage of the total atmospheric pressure, it remains the same, i.e. 20.95% of the total.
At sea level the partial pressure of O2 (pO2) in the atmosphere depends on many factors including the barometric pressure, the relative humidity (RH), air temperature & other prevailing factors such as wind, pollution, etc.
Relative humidity (RH) is a significant variable which often depends on local geography, e.g. a sea-side location or a land-locked one, wind direction, e.g. the prevailing winds passing over a body of water or over a hot, dry land mass, & season of the year, e.g. summer or winter.
Importantly, relative humidity changes can affect the water content of conventional hydrogel CL materials. A low relative humidity will ↓ the water content of a CL in situ. This will result in a ↓ in the availability of O2 under the CL because of the lowered Dk of the material resulting from dehydration.
Somewhat paradoxically, the standard atmosphere has 0% RH, an impossibility in reality. The partial O2 pressure in this dry standard atmosphere is 159 mm Hg, i.e. 20.95% of 760 mm Hg. This figure also appears in the literature.
While a standard atmosphere is defined, its component values are somewhat nominal because of the number & efficacy of the variables that can influence them. Although minor, even the latitude at which an atmosphere is measured has some influence.
The components of dry air are subject to less local variation (at sea level) (see pie chart representations earlier). The ‘water vapour over water’ vapour pressure, i.e. the saturated vapour pressure, varies with temperature (see above).

## Slide 10
标准大气
温度: 15 °C
气压: 760 mm Hg
水蒸气压@ 15 °C: 12.79 mm Hg
干性成分大气压: 747.21 mm Hg
氧浓度: 20.95%
氧分压 (pO2): 156.54 mm Hg
氧分压常用值: 155 mm Hg
氧分压(pO2)
Notes: The water vapour pressure over water (12.79 mm Hg) at 15°C, the temperature of the ‘standard atmosphere’, gives a nominal value which can be used to calculate a pressure of the dry atmosphere. From this result an O2 partial pressure (pO2) can be derived, i.e. 20.95% of the dry total. This is 156.54mm Hg. If the RH is 50%, the ‘water vapour pressure over water’ value should be halved & the pO2 recalculated (157.8 mm Hg).

## Slide 11
135
140
145
150
155
160
-10
0
10
20
30
40
50
@ 海平面
100% RH
50% RH
空气温度°C
氧分压 (mm Hg)
氧分压 vs 温度
Notes: This effect is shown graphically above. The graph appears to exaggerate the effect because of the range chosen for the y (pO2) scale.
For simplicity, a value slightly lower than calculated, i.e. 155 rather than 156.54, is used in most published works. The inaccuracy introduced is of the order of 1% which is of little practical consequence in the light of the variability of the actual value under real-world circumstances.
The most influential factor is altitude. The value 155 mm Hg is used as the O2 partial pressure at sea level in this lecture, as it is the value that has been used in the literature for many years.

## Slide 12
丹佛 (美国) 1,609 m
墨西哥市(墨西哥) 2240 m
库斯科 (秘鲁) 3360 m
马特洪峰(瑞士) 4476 m
德纳里峰(a.k.a. Mt McKinley, 美国) 6194 m
珠穆朗玛峰(a.k.a. Mt Everest, 泥泊尔) 8844.43 m (snowless, Chinese Acad of Sci., 2005)
0
200
400
600
800
0
5000
10000
15000
20000
大气压(mm Hg)
海拔高度 (米)
pO2
大气压
阿空加瓜山 (阿根廷) 6962 m
大气压vs 海拔高度
Notes: The effect of altitude on atmospheric pressure, & O2 partial pressure (pO2), is illustrated graphically above.

## Slide 13
‘有效氧% (相对于海平面)
0
5000
10000
15000
20000
氧分压 (mm Hg)
海拔高度（米）
氧气
丹佛 (美国) 1,609 m
墨西哥市(墨西哥) 2240 m
库斯科 (秘鲁) 3360 m
马特洪峰(瑞士) 4476 m
德纳里峰(a.k.a. Mt McKinley, 美国) 6194 m
珠穆朗玛峰 (a.k.a. Mt Everest) 8844.43 m
阿空加瓜山 (阿根廷) 6962 m
100%
10.8%
60.8%
34.2%
30.8%
155
94
53
17
48
0
氧分压vs 海拔高度
Notes: This theme is expanded above which plots the percentage (relative to that at sea level) & partial pressures of O2, against the altitude of various geographical features or inhabited areas from around the world.

## Slide 14
1升(@海平面) 气球 在不同的海拔高度
珠穆朗玛峰
8,844 m
1升气球 (@海平面)
在不同的海拔高度
相对空气密度
海拔高度（米）
Tn为绝对温度
Notes: Using standard equations it is possible to calculate the volume a gas would occupy under various atmospheric conditions. This slide shows the volumes & the apparent size (diameter) a 1 litre balloon (at sea level) would have at altitudes to 30,000 metres. The physical properties & influence of the balloon itself are assumed to be zero & are ignored.
The relative air densities are also shown graphically. Air temperature & altitude are not directly related, i.e. the air temperature does not simply get colder & real data has been used in the underlying calculations. The data for the highest point on earth, Chomalungma (Mt Everest) is shown for comparison. At Chomolungma’s peak, the atmospheric pressure is about 252 mm Hg of which 51-53 mm Hg is contributed by O2, i.e. the ‘effective’ O2 availability is approximately one third of the value at sea level. This implies that 3X the volume of ‘air’ would have to be inhaled on top of Chomolungma as would be inhaled at sea level, to access the same amount of O2. The effort required to do so is not sustainable & O2 masks are usually employed. There are other adverse responses to altitude by the body but these will not be dealt with here.
The cornea depends largely on the O2 available to it, rather than being able to ‘adapt’ by invoking an active process to compensate for O2 deprivation. This applies to the deprivation due to altitude as well as the deprivation due to the wearing of CLs.
In flight, commercial aircraft maintain cabin pressures much higher than the pressure outside the fuselage so as not to produce hypoxia and/or breathing difficulties in passengers. This process is called ‘pressurization’ & the cabin is said to be ‘pressurized’. Pressures of between 550 & 600 mm Hg, of which 115-126 mm Hg are due to the O2 component, are used normally. If the destination is located at high altitude less pressurization is applied to aid acclimatization on arrival (data from a member of the Aviation Medicine E-mail group, 1999).
A few studies have used similar artificial environments to simulate CL wear at high altitudes. Strath & Banister (1991) simulated conditions at 4267 metres & found twice the corneal swelling (8% versus 4%) & 3 of 7 subjects exhibiting vertical striae. Their results suggested a minimum O2 level of 12.2% is required to prevent significant corneal changes.

## Slide 15
大气
眼动脉分支供应
  前方
  角巩膜缘
  睑结膜
眼睛的氧气供应
Notes: 12
12

## Slide 16
角膜层次
睁眼
闭眼
上皮层
大气
房水？
睑结膜
球结膜?
房水?
基质层
房水
大气？
房水
内皮层
房水
房水
房水
虹膜血管
虹膜血管
角膜氧供的来源
Notes: Sources of Corneal O2
It has been suggested that almost the sole source of O2 for the epithelium is the atmosphere (in the open eye) & the palpebral conjunctival vasculature (in the closed eye).
Further, the endothelium is supplied solely by the aqueous humor (Weissman et al., 1981). Riley (1969) & Fatt et al. (1974) demonstrated a net flux of O2 from the anterior chamber into the cornea even in the open eye. This means that the endothelium is supplied by the aqueous humor even in the open eye, while in the closed eye it is dependent on this source (Fatt et al., 1974).
Hamano et al. (1986b, fig. 4 in article) showed that in the rabbit eye, when a PMMA CL is worn, the stromal pO2 is higher than the anterior corneal pO2. This suggests the anterior chamber as the source of O2, at least as far forward as the anterior stroma. A similar result had already been shown by Steffansson et al. (1983) in the cat. Their report showed that when an impermeable CL is worn, the O2 tension in the anterior chamber decreases due to an increased O2 flux into the cornea.
Zantos’ discovery of endothelial blebs in the in vivo cornea (see Zantos & Holden, 1977) also demonstrated that the endothelium is not entirely independent of the external eye environment, albeit by mechanisms unknown.
Endothelial blebs are changes in the appearance of the endothelial mosaic observed soon after the introduction of a contact lens, hypoxia/anoxia or experimental gases containing carbon dioxide in the presence of normal amounts of O2 (see Holden et al., 1985). This ‘influence’ of the external environment may not be O2-mediated however. It may be lactate mediated as first suggested by Riley (1969), the result of a pH decrease as suggested by Holden et al. (1985), or simply pH changes (Williams, 1986).
However, the endothelium & stromal keratocytes are almost solely dependent on the aqueous humor for O2. The other corneal components are not active metabolically. Riley (1969), suggested that in the rabbit eye at least, about 20% of corneal O2 was derived from the aqueous humor.
In the past, the source of aqueous humor O2 was assumed to be the ciliary body & the iris vasculature. More recently however, Hoper et al. (1989) showed that the source was probably just the iris vasculature.
This conclusion was reached after a comprehensive study of the pO2 values at many places in the anterior chamber adjacent to the iris itself, in rabbits & monkeys. The values in front of the pupil were very low, & were much higher in the periphery. Further support for their claim was provided by a repetition of their measurements following partial & complete iridectomies.

## Slide 17
海拔高度
接触镜
硬镜, 水凝胶, 硅水凝胶, 小巩膜镜, 巩膜镜
  材料 (Dk [Dk/t ])
  厚度 ( t [Dk/t ])
  配适 (紧, 正常, 松, 平坦, 陡峭, 等.)
角膜氧供:影响因素
Notes: 12
12
Determinants of O2 Supply to the Cornea
O2 tension levels vary across the cornea & within the cornea. The highest level is at the anterior surface. This is perhaps fortunate because the epithelium is the most metabolically active of the cornea’s layers & its structural & functional integrity is critical to its barrier function.

## Slide 18
注释: 厚度不成比例
无镜片
‘有效氧%
氧分压 (mmHg)
前弹力层
后弹力层
内皮层
基质层
上皮
40
80
120
160
55
0
5
20.95
0
泪膜
10
15
睁眼
闭眼
(after Benjamin, 1994)
角膜氧供: 分布– 无镜片
Notes: The O2 tensions & percentage distributions across the corneal layers are shown above for the following:
Open eye, central
Closed eye, central
The O2 tension at the superior anterior surface of the cornea is ↓ by the presence of the eyelids to an extent that varies from individual to individual.
Behind closed eyelids, atmospheric O2 is unavailable. Under closed eye conditions O2 to the anterior eye is supplied from the palpebral conjunctival vessels principally, the bulbar conjunctiva & minimal amounts from the limbal vasculature.
Since the driving force of the O2 supply to the anterior eye is atmospheric pressure, the reduced availability at high altitudes (reduced partial pressure) means the amount of O2 absorbed is reduced & the level in corneal tissue is lower.
The wearing of CLs reduces the supply of O2 to the cornea. The type of contact lens, i.e. GP or SCL, as well as CL factors such as material & thickness affect the flow of O2 to the cornea. All result in a lower O2 supply to the anterior surface of the cornea.

## Slide 19
角膜氧供: 分布 – 配戴不同镜片
Note: Thicknesses not to scale
氧%
氧分压(mmHg)
40
80
120
160
55
0
5
20.95
0
接触镜
10
15
A
B
D
C
前弹力层
后弹力层
内皮层
基质层
上皮层
(after Benjamin, 1994)
Notes: This slide shows the O2 tension & percentage distribution across the corneal layers for CLs that allow the following O2 tensions at the central anterior surface:
Lens A – 15%
Lens B – 10%
Lens C – 5%
Lens D – 0%
The fitting characteristics of a CL may also play a rôle, albeit minor, in O2 supply. Whether rigid or flexible, any CL that permits a greater exchange of tears with each blink will provide more O2 than a CL that is ‘tight’ and/or immobile on the cornea.
Typically, the contribution of fit to corneal oxygenation is much more significant with GP lenses. Fatt & Lin (1976) & Decker et al. (1978) showed that the ‘tear pump’ under SCLs was a minor contributor to corneal oxygenation. Using a fluorophotometer, Polse (1979) showed that when SCLs were worn, each blink only exchanged about 1.1% of the tear volume. On the other hand, GPs exchange some 10 to 20 times this amount.
Recently, these figures were confirmed in a study by McNamara et al. (1999). Their study, again using fluorophotometry, showed exchange rates of between 1.24% & 1.82% per blink when SCLs were worn. Interestingly, smaller SCLs (TD: 12 mm) resulted in greater exchange rates but even these CLs only gave ‘modest’ results when compared with GP CLs.
However, tear exchange is only a part of a larger scenario. Once other critical factors such as O2 permeability (Dk), CL thickness, area of cornea covered, etc. are taken into account, GP CLs deliver approximately 3X more O2 to the cornea than SCLs (Mandell et al., 1987). Silicone hydrogel (SiHy) CLs are much better (6-10X) than SCLs.
Developments since this finding including higher permeability materials, have probably increased the lead GP materials currently enjoy. The now mature SCL category of siloxane & fluoro-siloxane-containing low-water hydrogels whose Dks can match or exceed those of GP materials, reduce, or even eliminate, the margin once enjoyed by GP materials despite the latter not covering all of the cornea.

## Slide 20
氧分压的研究包括：
角膜不同部位
睑结膜囊和眼睑
基质
内皮
不同部位的房水
研究采用：
人类
兔子
猫
猴子
氧含量水平
Notes: Ocular O2 Levels: Open & Closed Eye
The O2 tensions (partial pressures) at various points in the eyes of several animal species have been measured or estimated. The results are often based on assumptions extrapolated from in vitro data & may be method-dependent.
An atmospheric pressure of 760 mm Hg at sea level is assumed. Therefore, in the open eye, the anterior corneal surface is exposed to a partial O2 pressure (pO2) of 155mm Hg (derived previously).
Many papers draw attention to the significant individual variation found in the pO2 levels and/or O2 consumption rates measured for both animal & human studies, e.g. Mandell & Farrell, 1980, Holden et al., 1984, Lin, 1992. Lin also suggests that the O2 consumption rate varies over time within an individual.
The published open-eye O2 tensions at various levels of the anterior eye are summarized next.

## Slide 21
位置
人
兔子
猫
眼睑下
33.7 – 61.4
38.9
镜片下
0 – 82.3
0.58 – 112
前房
50 – 59.7
7.7 – 65
30 - 37
戴镜时前房
25 - 75
6 – 27.73
13
氧分压数据汇总: 睁眼
分压单位：mmHg
Notes: Summary of Published pO2 Data
All Species:
At the anterior ocular surface:
151 to 159 mm Hg
(Benjamin & Hill, 1988, Benjamin, 1994, differences partly due to laboratory altitudes).
Open eye, HUMAN:
Under the lids:
33.7 to 61.4 mm Hg
Under CLs:
0 to 82.3 mm Hg
In the anterior chamber:
40 to 59.7 mm Hg
In the anterior chamber , CLs on:
25 to 75 mm Hg
(Benjamin, 1994, Hamano et al., 1986, Serdahl et al., 1989, Efron & Carney, 1979, Holden & Sweeney, 1985, Fatt et al., 1974, Weissman, 1986, Polse & Decker, 1979, Rasson & Fatt, 1982, Hamano, 1985, O’Neal et al., 1983, Friedenwald & Pierce, 1937, Kleifield & Neumann, 1959, Fatt & Bieber, 1968, Fatt, 1978, Ruben, 1975, Benjamin, 1994, Thiel, 1967, Fatt & Ruben, 1993)
Open eye, RABBIT:
In the conjunctival sac:
38.9 mm Hg
Under CLs:
0.58 to 112 mm Hg
In the anterior chamber :
7.7 to 65 mm Hg
In the anterior chamber, CLs on:
6 to 27.73 mm Hg
(Hamano et al., 1986, Fatt & Lin, 1985, Hamano, 1985, Ichijima et al., 1998, Harvitt & Bonanno, 1996, Kwok, 1985, Kleinstein et al., 1981, Stefansson et al., 1987, Barr & Roetman, 1974, Barr & Silver, 1973, Hoper et al., 1989, Kleinstein et al., 1981, Stefansson et al., 1983, Mc Laren et al., 1998)
Open eye, CAT:
In the anterior chamber :
30 to 37 mm Hg
In the anterior chamber with PMMA CLs on:
13 mm Hg
(Fatt et al., 1982, Kwok, 1985, Stefansson et al., 1983)
Open eye, monkey:
pO2 anterior chamber :
41.5 to 13.9 mm Hg depending on sensor position
(Hoper et al., 1989)

## Slide 22
位置
人
兔子
眼睑下
50 - 67
镜片下
0 - 35
前房
55
8.7
戴镜时前房
5.1 – 12.9
氧分压数据汇总: 闭眼时
分压单位：mmHg
Notes: Closed-eye, HUMAN:
At the central cornea:
50 to 67 mm Hg
In the anterior chamber:
55 mm Hg (Ruben, 1975).
Under CLs:
0 to 35 mm Hg
(Kwan & Fatt, 1970, Benjamin, 1982, Fatt & Bieber, 1968, Fatt & Lin, 1985, Fatt, 1987, Benjamin, 1994, Ruben, 1975, O’Neal et al., 1983, Ichijima et al., 1998)
Closed-eye, RABBIT:
In the anterior chamber:
8.7 mm Hg
In the anterior chamber, GP CLs on:
5.1 to 12.9 mm Hg
(Barr & Silver, 1973, Hamano et al., 1986)
Anterior anoxia, human:
Under lid:
42.8 mm Hg
(Efron & Carney, 1979)
Anterior anoxia, rabbit:
pO2 anterior chamber:
9.6 ±2.9 mm Hg
(Barr & Silver, 1973).

## Slide 23
固有的材料特征(组织气体通过)
透氧性P = Dk :
  D =扩散系数
  k = 该材料的溶解系数
角膜的氧供: 接触镜的透氧性
Notes: 12
12
O2 Supply to the Cornea with CLs
As O2 is required to maintain the cornea’s normal metabolic activity & structural integrity, a key factor in the success of CL wear is the provision of an adequate supply of O2 to the cornea.
All CLs ↓ the amount of O2 available to the cornea. In most cases, this reduction has only a minimal impact. However severe problems can occur in both the short & long-term should the O2 availability fall well below the critical level required for on-going corneal health.
CL wear exacerbates the phenomenon of lowered O2 availability that occurs during eye closure. Further, corneal temperature has been shown to rise in the closed eye by about 3 °C. ↑ corneal temperatures have been associated with ↑ in the anterior cornea’s rate of metabolic activity (Freeman & Fatt, 1973).
Therefore, the use of CLs in the closed eye presents a physiological challenge to the cornea because of the ↑ temperature (largely not CL related) & ↓ O2 availability (a routine factor in eye closure exacerbated by the presence of CLs).
O2 Permeability of CL Materials
O2 permeability (Dk) is an intrinsic physical property of the material from which a CL is fabricated. The diffusion coefficient (D) defines the speed of movement of the gas molecules within the material. The solubility coefficient (k) defines the number of O2 molecules dissolved in the material (Fatt, 1992).
The permeability (Dk) varies directly with temperature, i.e. the higher the temperature, the greater the Dk. For most calculations a temperature of 34 °C is used, as this approximates the corneal temperature in the open eye.
A CL material’s O2 permeability is a calculated value that provides a useful guide in clinical applications. In order to determine the Dk it is necessary to first do an in vitro test to measure the O2 transmissibility (Dk/t) of a CL fabricated from it. This value is then multiplied by the thickness (t) to obtain the Dk.

## Slide 24
隐形眼镜材料
O2
输入
输出
透氧性: D
Notes: O2 permeability is given the symbol Dk. The first term, D, is the diffusion coefficient of the CL material & is a measure of the VELOCITY of gas molecules moving in the material. Unfortunately, because of the randomness of the gas molecules’ movement in the material, velocity is measured as an AREA moved, rather than the more traditional distance moved, in unit time (seconds), i.e. cm2/sec. Some gas molecules pass directly or nearly so through the CL material while others are deflected after entering the material & take a much less direct path before exiting the material. In some materials the molecules can actually move backwards & exit the material from the same surface they entered. Direct passage leads to an apparently high velocity whereas indirect or backward movement lead to a low apparent velocity. If most of the gas molecules fail to make it through or most exit from the surface they entered, then the apparent velocity is low or nearly zero (after Fatt, 1995).
Fatt I, 1995. Oxygen Transmission. Chapter 7A. In: Kastl PR Ed., Contact Lenses The CLAO Guide to Basic Science and Clinical Practice. Kendall/Hunt Publishing Company, Dubuque.

## Slide 25
接触镜材料
O2
k = 溶解系数
(氧气在接触镜材料中的溶解度)
高溶解
不溶解
可溶解
透氧性: k
Notes: The second term, k, is the material’s SOLUBILITY coefficient & is a measure of how much gas can be dissolved in the material (think of water in a sponge). The k value is expressed as the number of mL of O2 dissolved in 1 mL of the CL material for each mm (Hg equivalent) of atmospheric pressure acting on the material (mLO2/(mLMat X mmHg).
Traditionally, STP (Standard Temperature & Pressure) is used in science but in relation to CL technology either 20 °C (a moderate-climate average room temperature) or 34 °C (a widely-accepted corneal temperature) is used.
Therefore: Dk = [cm2O2 / sec] X [mLO2/(mLMat X mmHg]
= cm2O2 / sec X mLO2/(mLMat X mmHg)
(after Fatt, 1995).
Fatt I, 1995. Oxygen Transmission. Chapter 7A. In: Kastl PR Ed., Contact Lenses The CLAO Guide to Basic Science and Clinical Practice. Kendall/Hunt Publishing Company, Dubuque.

## Slide 26
材料的氧溶解度： 非常 高
O2
O2
接触镜材料
O2
氧气通过材料:
快速, 直接, & 无阻碍
O2
透氧性: 各部位都想要什么？
Notes: What is sought by all concerned is a material with a very high Dk. This can only be achieved by both D & k being very high.

## Slide 27
与材料厚度无关(t )
与温度有关(T °C)
计算值
透氧性
Notes: 12
12
A knowledge of a material’s Dk allows the practitioner to design, or select a stock design of, a CL that will provide an adequate supply of O2 to the cornea. This is especially the case when deciding on CL centre thickness because of its effect on CL transmissibility.
Where the O2 permeability of a CL is to be measured, the CL must have parallel front & back surfaces, i.e. in the interests of having the influential central zone thickness uniform, the FOZR & BOZR should differ by the CL thickness only (FOZR–BOZR = tc).
Powered CLs should be avoided because of the complexity introduced by the topographical variation in their thickness. However, it is noteworthy that a CL with parallel surfaces has a small amount of negative power.
Examples:
SOFT: GP:
FOZR : 8.9 mm FOZR:7.9 BOZR : 8.8 mm BOZR: 7.8 tc : 0.1 mm tc: 0.1 mm n : 1.399 n : 1.43 BVP : –0.37D BVP: –0.49
(FOZR Plano: 8.83 mm FOZR Plano: 7.83 mm)

## Slide 28
Dk =
mmHg
x
mL
x
s
mL
x
cm
镜片
O
2
2
k =
mmHg
x
mL
mL
镜片
O
2
D =
s
cm
2
&
Dk =
mmHg
x
mL
mL
X
s
cm
镜片
O
2
2

透氧性: 单位
Notes: O2 Permeability: Units
The unit of O2 permeability (Dk) is derived from the diffusion coefficient D & the solubility coefficient k (above).
D, the diffusion coefficient, defines the velocity of O2 gas molecules moving in the CL material. The ‘velocity’ of randomly moving gas molecules diffusing through a material is expressed in terms of an area per second, i.e. cm2/s rather than the more conventional cm/s that applies to non-gaseous entities (Fatt, 1995).
k, the solubility coefficient, defines the volume of O2 that can be dissolved in the CL material (after Fatt, 1995). k is expressed in terms of the volume of O2, the volume of CL material & the pressure driving the O2 into, & through, the CL material, i.e. mLO2/(mLLens x mm Hg).
(Note: millilitres (mL) & cubic centimetres (cm3) are used interchangeably here. However, they are not exactly the same due to a minor error in the early definition of the litre. Strictly, 1 litre (L) is the volume occupied by 1 kilogram (kg) of pure water at the temperature of its maximum density (approximately 3.984 °C [2004 value]). More accurate measurements made subsequently, showed that this volume was actually 1.000028 cubic decimetres ([10 cm]3). Therefore, one mL is fractionally smaller than 1 cm3 but the inaccuracy is only of the order of 1 in 36,000 (Jerrard & McNeill, 1992).

## Slide 29
镜片材料
1 cm
1 cm
1 cm
after Refojo et al., 1984
1 秒
1 mm Hg 压力
1 cm
1 cm
1 cm
O2
1 cm
1 cm
1 cm
O2
假设的接触镜 (比真实接触镜大很多)
情况: STP (0 °C, 760 mm Hg) 除非注明，否则为, 21 or 34 °C @ 760 mm Hg
透氧性: 单位
Notes: A graphical concept of the Dk unit is presented in the slide above. In this slide, 1 cm3 of O2 is being driven through 1 cm3 of polymeric CL material (any type) by a positive partial pressure of O2 (pO2) difference across the CL of 1 mm of mercury pressure in 1 second under a stated set of environmental conditions.
While the atmospheric pressure is usually assumed to be 760 mm Hg, the temperature must be stated because the Dk is temperature sensitive. This is largely because the level of gas molecule activity (agitation) ↑ with temperature. Increased activity ↑ the success rate of gas molecules entering, & eventually passing through, a CL polymer. This slide is a purely theoretical representation for illustration purposes only. Real CLs contain nothing like the volume of polymer implied here, nor are driving pressures as low as 1 mm Hg; O2 volumes as high as 1 cm3; & the time involved as short as 1 second.

## Slide 30
接触镜DK范围: 0 - 300 x 10–11
单位:
  (cm2 x mLO2) / (s x mLlens x mm Hg)
  or
  (cm2/s) x (mLO2 / [mLlens x mm Hg])
  通常，下标lens 常省略
透氧性
Notes: 12
12
Estimates of human corneal O2 consumption vary between 1.6 & 10.9 mL per cm2 of cornea per hour (Efron & Brennan, 1992). Realistic measures result in an exponent of 10–11 being appended to the Dk unit (see slide). Furthermore, in many instances in which Dk units are presented, the lack of brackets or statements of mathematical processing precedence lead to potential confusion as to which components of the unit form the numerator (top) & which form the denominator (bottom).
More recently, Alvord et el. (1998) have suggested that an historic unit of O2 permeability, the barrer, be used as an alternative to the widely used, but somewhat cumbersome 10-11 (cm2 x mLO2)/(s x mLLens x mm Hg). They argue that by using the barrer for permeability & the more traditional unit for transmissibility, i.e. 10-9 (cm x mLO2)/(s x mLLens x mm Hg), confusion between the two can be reduced. To date, the barrer has only gained some acceptance.

## Slide 31
与材料的透氧性有关(Dk)
与材料的厚度有关(t)
  氧传导性 = Dk/t
有临床性意义
透氧性
Notes: 12
12
O2 Transmissibility of CLs
The O2 transmissibility of a CL is a physical property of the actual lens, i.e. a property of both its material & its thickness. It is equal to the material’s O2 permeability divided by the CL thickness, i.e. Dk/t.
The exponent 10–9 is appended to the unit of transmissibility because CL thickness is expressed in centimetres (cm), e.g. a thickness of 0.1 mm is 0.01cm. It is normally specified at a specific temperature, usually 34 °C, sometimes 35 °C.
The permeability, & therefore the transmissibility, are temperature dependent & are related directly, i.e. the higher the temperature, the higher the Dk & therefore the higher the Dk/t. Because of the greater relevance of an on-eye temperature, such figures are probably more useful clinically. Alternatively, an in vitro laboratory temperature may be quoted. This is usually 20 or 21 °C.
Clinically, O2 transmissibility is more useful than O2 permeability as it relates directly to on-eye issues as it includes CL thickness.
Commonly, the transmissibility of a CL series is given for a CL BVP of 3.00 D, a BVP that has become something of a de facto industry standard.
However, it is important to realize that the value stated varies according to CL BVP because of the latter’s effect on CL thickness at any point within the optic zone and the blend to the lens periphery just outside the optic zone. A CL of plus power has significantly less transmissibility at its centre than does a minus powered lens. The Dk/t of a minus CL has little relevance to a plus lens, especially one of significant plus power.

## Slide 32
氧传导性: 单位
Dk =
mmHg
x
mL
x
s
mL
x
cm
Lens
O
2
2
Dk/
t
=
cm
x
mmHg
x
mL
x
s
mL
x
cm
Lens
O
2
2
Dk/
t
=
mmHg
x
mL
x
s
mL
x
cm
Lens
O
2


## Slide 33
镜片范围: 0 - 200 x 10–9
单位:
  (cm x mLO2) / (s x mLLens x mm Hg)
  or
  (cm/s) x (mLO2/ [mLLensx mm Hg])
  通常，下标Lens常省略
氧传导性
Notes: 12
12

## Slide 34
不配戴接触镜
经验配戴者vs 新手
日戴型(DW)
长戴型(EW)
镜片设计/材料特征
角膜氧供和接触镜配戴: 角膜需氧量 – 一般
Notes: 12
12
CLs & O2 Transport to the Cornea
A major goal of CL material research & development is to increase material O2 permeability to boost the levels of O2 available to the cornea during CL wear.
Breakthroughs in the polymer chemistry of hydrogels, siloxane elastomers, SiHys, & rigid gas permeable CL materials have resulted in CLs that offer a wide range of O2 transmissibilities.
As advances yield higher O2 performances, older materials that offer no special advantages or characteristics are deleted from product lines. Particularly in the case of GP CL materials, this means that current product lines range from average to high performance rather than low to average.
Issues not related to O2 which may help a less permeable material remain attractive to users include economic pricing, ease of manufacture, stability of parameters when worn, & surface wettability in situ.
Corneal O2 Requirements: General
To understand the effects of CLs on the structure & function of the cornea, it is necessary to consider its normal O2 requirements under a variety of conditions both with & without CLs.
The major questions are:
What is the minimum level of O2 required by the cornea to maintain normal metabolic activity?
Does the corneal O2 demand change with CL wear?
What effects do the different wear modalities have on the cornea’s need for O2?
How do the variables of CL material & design affect corneal O2 supply during CL wear?

## Slide 35
临界氧气水平
Holden-Mertz 标准 (Dk/t) (DW & EW)
个体差异大
异常角膜:
    手术
    疾病
    创伤
角膜氧供和接触镜配戴: 角膜需氧量
Notes: 12
12
Corneal O2 Requirements: Definition
Many researchers have attempted to measure & define the minimum amount of O2 the cornea needs to maintain successful CL wear.
These studies have investigated numerous phenomena associated with CL wear including:
Corneal swelling
Structural changes
Biochemical changes
Alterations to cell reproduction
Changes in corneal sensory behaviour.
Polse & Mandell (1971) conducted one of the earliest studies that attempted to define the critical O2 requirements of the cornea. The major study in this field is that of Holden & Mertz (1984). Holden & Mertz attempted to define the minimum CL O2 transmissibility required to meet the needs of various modes of CL wear. Their assessment of need was based on the levels of corneal swelling (corneal oedema) measured by optical pachometry (pachymetry).
Their study, which was derived from a series of large clinical studies, provided valuable information on the average human corneal O2 requirement.
However, it is important to note that because of significant individual variation, many CL wearers require more corneal O2 than the average to maintain normal corneal function, while others may need less. Only wearers in the former category are a concern clinically.
Consideration must also be given to the O2 needs of the cornea that has undergone surgery or been affected by a disease process (Holden et al, 1980).
More details on the critical O2 requirements according to various physiological criteria, & the effects of hypoxia on the cornea, are given in Lecture 6.1, Section IV of the original ICLC.

## Slide 36
白天无角膜水肿:
  Dk/t = 24.1 ± 2.7 x 10–9
  EOP* 为9.9%
角膜氧供和接触镜配戴: 角膜需氧量 – 软镜日戴
Notes: 12
12
O2 Requirements During SCL Daily Wear
Physiologically, the ideal SCL, when worn on a daily wear (DW) basis, should cause zero corneal oedema (swelling). To minimize its impact on the average cornea, the O2 transmissibility of a SCL should be 24.1 ± 2.7 x 10-9 units based on the study of Holden & Mertz (1984).
Alternatively, this O2 requirement can be expressed in terms of the equivalent O2 percentage (EOP*) required at the corneal surface (EOP has fallen out of favour for technical and practical reasons – see below). For a SCL to induce zero swelling during DW, the EOP value should be 9.9% for the ‘average’ cornea.
* Equivalent Oxygen Percentage (EOP). An early measure of assessing the physiological performance of a CL. A cornea’s response (O2 demand as determined by an O2 electrode applied directly to the bare cornea) to a rational series of gas mixes of known O2 partial pressure is used to create a ‘calibration’ curve of electrode response versus the level of hypoxia. After a CL has been worn for some time (stable circumstances under the CL reached) the CL is removed & an O2 electrode is applied immediately to the exposed cornea. The O2 consumption rate is then used to estimate the equivalent gas mixture (pO2) that would have resulted in the same consumption rate just measured (from the ‘calibration’ curve). Essentially, the CL produces an O2 debt that is measured indirectly by the electrode. The technique has fallen into disfavour as it has been shown to be unreliable, unpleasant, limited largely to research laboratories, & too indirect (& subject to too many vagaries in its application) to be used as a measuring standard. Furthermore, the advances & refinements in in vitro assessments of CL physiological properties have resulted in more rigourous, more accurate, & more reliable methods eclipsing the relatively cumbersome and time-consuming EOP method.

## Slide 37
–1
0
1
2
3
4
5
6
7
8
9
10
0
10
20
30
40
计算 Dk/tavg
(cm x ml O2 / 秒 x ml x mm Hg)
角膜水肿(%)
Dk/tavg = 24 x 10–9
r = – 0.96
DW
角膜氧供和接触镜配戴: 角膜水肿vs Dk/t
Holden & Mertz, 1984
Notes: 12
12
Graph representing lesser corneal oedema with the CL materials having higher O2 transmissibility (Dk/t) values

## Slide 38
闭眼戴镜，无角膜水肿:
  Dk/t = 34.3 ± 5.2 x 10–9
  EOP* 为12.1%
角膜氧供和接触镜配戴: 角膜需氧量– 软镜，长戴
* See Notes
Notes: 12
12
O2 Requirements During SCL Extended Wear (EW): Zero Residual Swelling
Following overnight wear of an SCL, the cornea swells by an amount which is related to the O2 transmissibility of the material. After eye opening, the cornea begins to thin as its metabolic activity ↑ due to the higher availability of O2.
Holden & Mertz (1984) determined the SCL O2 transmissibility required to permit the cornea to return to baseline corneal thickness (no residual daytime oedema) prior to the next period of eye closure, when CLs are worn on an EW basis.
According to their calculations, the O2 transmissibility of an SCL must be 34.3 x 10-9 units or an EOP of 12.1%. This Dk/t value limits the permissible overnight corneal swelling to approximately 8.0%.

## Slide 39
过夜角膜水肿= 4.0%
  Dk/t = 87.0 ± 3.3 x 10–9
  EOP* of 17.9%
角膜氧供和接触镜配戴: 角膜需氧量 – 软镜，长戴
Notes: 12
12
O2 Requirements During SCL EW: Maximum of 4% Overnight Swelling
Physiologically, the ideal SCL for EW is one that produces no more corneal swelling than a non-CL wearing eye following 8 hours of sleep. The normal, no-CL overnight corneal swelling is of the order of 4.0% (the literature provides figures between 3% & 5.5%).
To achieve this, the O2 transmissibility of an SCL must be 87.0 x 10-9 units or an EOP of 17.9% (Holden & Mertz, 1984).

## Slide 40
Holden & Mertz, 1984
0
10
20
0
10
20
30
40
Dk/t平均 (cm x ml O2) / (秒 x ml x mm Hg)
角膜水肿(%)
Dk/tavg = 87 x 10–9
15
5
140
130
//
长戴
角膜氧供和接触镜配戴: 过夜角膜水肿vs Dk/t
Notes: More recently, this topic has been re-examined by Harvitt & Bonanno (1999) using a model incorporating their finding that ↑ corneal O2 consumption results from corneal acidification (Harvitt & Bonanno, 1998).
For humans, they found the minimum CL transmissibility that would deliver O2 to the basal epithelial cells was 23 (X10–9) for the open eye & 89 (X10–9) for the closed eye. These figures agree very closely with Holden & Mertz (1984) estimates (24 & 87 respectively).
To prevent anoxia across the entire corneal thickness, Harvitt & Bonanno (1999) suggested transmissibilities of 35 (X10–9) for the open eye & 125 (X10–9) for the closed eye are required.
These figures represent a new ‘high-water mark’ in the estimates of the O2 minima required to prevent hypoxia-related adverse corneal responses. The latest generation of GP & SiHy materials can deliver these levels, whereas previous generation materials could not.

## Slide 41
镜片下泪液交换率:
  软镜 1% 每瞬目一次
  硬镜 15 - 20% 每瞬目一次
瞬目
  频率
  质量(是否完全)
硬镜与软镜的配适特征
角膜氧供和接触镜配戴: 动态氧气供应
Notes: 12
12
CL Dynamics & O2 Supply
Measurement of O2 transmissibility provides an indication of the amount of O2 that will pass through the bulk of the CL to the cornea.
However, it is also important to assess the tear exchange behind a CL, as O2 also reaches the cornea in the tear fluid. This issue is covered in Lecture 6.1, Section I.B of the original ICLC.
SCLs have only minimal tear exchange with each blink due to their large total diameter & conformity with the corneal, & conjunctival surface shapes (Polse 1979). Parrish & Larke (1981) also showed that not only was the SCL tear pump ‘small’ but that it also varied slightly with CL fit. Consequently, the O2 transmissibility of the CL is the principal determinant of the supply of O2 to the cornea for SCLs.
On the other hand, rigid gas permeable (GP) CLs can supply significantly more O2 to the eye than SCLs via the exchange of tears that occur with each blink. Their greater tear exchange is due to their smaller total diameter, & greater on-eye movement.
It is estimated that 10-20% of the tear film behind an GP CL is exchanged for fresh, oxygenated tears following a blink.
Therefore, in GP CL wearers the blink rate, the completeness of each blink, & the CL transmissibility are all important determinants of corneal oxygenation.

## Slide 42
聚合物的形成
温度影响
镜片表面的氧分压
镜片厚度 ( t )
边界效应
角膜氧供和接触镜配戴: 透过接触镜的气体运动
Notes: 12
12
Gas Movement Through CLs
Five major parameters dictate the O2 permeability of a CL material.
The most important of these parameters is the composition of the polymer from which the CL is fabricated.

## Slide 43
分子通过材料体中的 微孔(分子间隙)移动
角膜氧供和接触镜配戴: 气体扩散
Notes: 12
12
Gas Diffusion
Diffusion is the process by which gas molecules (or molecules of other substances), move within another gas (or liquid or solid) to fill uniformly, all of the available space. This is made possible by the continuous random movement (Brownian movement in fluids, i.e. liquids and gases) exhibited by all molecules whose temperature is above absolute zero, i.e. 0°K or –273.15°C. At absolute zero (only approximated but not realized to date) all motion would cease & any diffusion would be suspended.

## Slide 44
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
渗透膜
The Ball & Hill Analogy
浓度 (高度)
(膜)
角膜氧供和接触镜配戴: 浓度梯度
Notes: When the concentration of a substance, or substances, is higher in a particular region of an enclosed space, the number of molecule collisions in this region is greater. This leads to a tendency for the molecules to distance themselves uniformly within the space, over time. In this situation, the least number of collisions occur, i.e. a state is reached in which the least amount of energy is ‘expended’ on collisions.
Similarly, when a concentration gradient exists across a membrane, there will be a tendency for the molecules to pass from the region of higher concentration towards that of lower concentration until such time as the concentrations are equalized (see slide).

## Slide 45
渗透膜
渗透膜
渗透膜
可渗透的
半渗透的
不可渗透的
角膜氧供和接触镜配戴: 渗透率
Notes: However, some membranes can resist (limited permeability) or even prevent (impermeable) the transfer of molecules. Some are somewhat selective in that they allow some molecular species to pass while denying passage to others, i.e. they are said to be semi-permeable (see slide).
If the membrane is permeable to the substance in question, molecules do not only pass in one direction, rather the net effect is as if the flow is unidirectional. This is because the activity of molecules on the lower concentration side results in some of the molecules travelling against the concentration gradient.
However, for each molecule travelling against the gradient, many more travel with the gradient because of the greater collision frequency in the space of greater concentration. This results in a net flow from the space of higher concentration to that of the lower concentration.
Ultimately, an equal number of molecules are passing in either direction, i.e. a state of equilibrium is reached. This can only occur when the concentrations on either side of the membrane are equal.
Gas molecules colliding with the membrane molecules can result in a failure to penetrate the membrane at all, or a more circuitous route being taken because of deflection or reflection of the molecule from its original trajectory.
In summary: when a membrane separates a mixture of gases, the molecules in greater concentration are propelled by their kinetic energy (molecular movement), & the resulting collisions, into & then across the membrane to the side with the lower concentration (after Refojo et al., 1984).
The transfer rate depends largely on the concentration gradient (differences in partial pressures), temperature (affects level of molecular agitation), & the properties of the membrane itself.
A gas can diffuse into & through a CL material if the molecules of the gas are able to find (& fit through) ‘voids’ (polymer-free spaces) (Hill, 1978) or ‘microvoids’ within the structure (Caroline & Ellis, 1986).
An example of this process occurs when a tennis ball is removed from its pressurized storage can for the first time. When manufactured, the pressure within the can is greater than that inside the ball, the ball will be compressed somewhat & the air trapped inside the ball cannot escape. Over time, the pressure inside & outside the ball will equalize by the pressurized air inside the can entering the ball. After opening the can, the air inside the ball diffuses through the micropores, or voids, within the rubber shell. In this way the ball eventually loses its bounce & becomes ‘flat’ (pressure inside the ball will be atmospheric pressure only instead of being higher than atmospheric prossure).
Each material (solid, liquid, or gas) has an inherent property called a diffusion coefficient that is given the symbol D. It is the D in the equation for O2 permeability, P= Dk. For details of k & P see the next slide & Notes text.

## Slide 46
气体在材料内部的吸收过程
类似于海绵吸水
气体溶解入材料中
角膜氧供和接触镜配戴: 气体溶解度
Notes: 12
12
Gas Solubility
The process of gas solubility in a CL can be likened to a sponge that absorbs & holds a liquid (Caroline & Ellis, 1986).
A CL material has a specific solubility coefficient that is given the symbol k in the O2 permeability (P) equation.
P = Dk
Because of the practical difficulties in measuring k, it is usual to measure the quantity Dk directly rather than by multiplication of its components (D & k) (Fatt, 1976).

## Slide 47
硅键(Si-O-Si)  分子微孔
键的大小、旋转和弹性会影响渗透率
浓度梯度
角膜氧供和接触镜配戴: GP材料的透氧性
Notes: 12
12
O2 Permeability of Rigid Gas Permeable CLs
Most GP CL materials contain siloxane, a generic name for chemical entities involving the silicon to oxygen bond (Si-O-Si), also referred to as the siloxane bond.
Such a bond is capable of rotation & flexure (including significant extension & compression) (see next slide).
During movement, molecular-sized spaces that permit the permeation of gases are formed within the material. Although these spaces exist only momentarily, they are open long enough to enable O2 molecules to pass (diffuse). They should not be regarded as ‘holes’. Rather, they should be viewed as potential voids (Caroline & Ellis, 1986). The degree to which this process occurs in a material is referred to as the diffusion coefficient (D) in the O2 permeability equation P = Dk.
A concentration gradient is formed across the CL thickness, i.e. between the front & back surfaces of the CL in situ, due to the consumption of O2 from the post-CL tear film by the cornea (or cornea & anterior eye in the case of SCLs). O2 passes along this gradient, through the lens, towards the eye to supply the anterior cornea via the post-CL tear film.

## Slide 48
甲基团小
甲基团没有极性而可以活动
硅原子间的距离大
大的无聚合物空间
聚合物主链是有弹性的 (可延伸的)
主链
压缩的
松的
延伸的
O
CH3
Si
CH3
O
O
130°
可延伸
的主链
CH3
Si
CH3
Si
甲基团能在硅原子周围自由旋转
角膜氧供和接触镜配戴: 硬性透气性材料硅氧烷成分

## Slide 49
三步过程:
  气体溶解入镜片前表面
  透过镜片微孔扩散
  气体离开镜片后表面，进入泪液
角膜氧供和接触镜配戴: GP材料透氧性
Notes: 12
12
The diffusion of O2 through the material is only one component of CL permeability. The value k in the permeability equation relates to the solubility of O2 in the material. O2 has a demonstrated preference for dissolving in fluorinated siloxane acrylates (FSAs) rather than siloxane acrylates (SAs).
The solubility of O2 within an GP material starts with the adsorption of the gas (O2) onto the front surface of the lens. The O2 then dissolves into the CL material through which it passes (diffuses) towards the back surface under the influence of the concentration gradient explained previously. It then leaves the back surface & enters the post-CL or pre-corneal tear film again by a further process of dissolution.

## Slide 50
透氧性是分子运动和/或溶解的功能
透氧性增加:
  增加表面特性
  增加温度
  减少交联
  增加大气压
聚合物成分
角膜氧供和接触镜配戴:GP材料透氧性
Notes: 12
12
The factors that determine the O2 permeability of an GP CL are:
Polymer composition
Temperature
Partial pressure at the anterior surface
Boundary layers (lens/tear film interface).
Polymer chemists who develop GP materials must ensure that certain desirable characteristics are not compromised in an attempt to develop a higher level of O2 permeability. Such characteristics include:
Rigidity
Durability
Wettability
Machinability
Long-term stability.

## Slide 51
丙烯酸酯 (PMMA)
硅氧烷 丙烯酸酯
氟-硅氧烷
丙烯酸酯
溶解氧
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
O2
角膜氧供和接触镜配戴: GP材料氟组件
Notes: Permeability of Fluorinated GP Materials
The SA (siloxane-acrylate) GP CL materials were developed further by the addition of a fluorinated monomer. FSAs (fluoro-siloxane acrylates) owe their higher O2 permeability to both their fluorine & siloxane components.
However, a siloxane bond provides a much greater level of O2 permeability than does the addition of fluorine, i.e. all other things being equal, the siloxane factor is more influential than the fluorine one.
While fluorinated CL materials are more O2 permeable due to the greater solubility of O2 in them (see slide), the major benefit of a fluorinated polymer is its improved surface properties compared with those of the SAs. The interaction between the CL & tear film components such as proteins, mucus, & lipids is ↓ significantly, resulting in ↓ deposits.
The combination of enhanced surface characteristics & higher O2 permeability makes the FSAs the materials of choice for the majority of patients who require, or elect to use, GP CLs.

## Slide 52
硅比氟更透氧
氟化聚合体有很好的表面特性
氟增加氧气在材料中的溶解
角膜氧供和接触镜配戴: GP氟化材料
Notes: 12
12

## Slide 53
材料透氧性 (Dk)
沉积物的作用小
接触镜厚度/BVP
瞬目后的泪液交换
隐形眼镜下的泪液厚度
角膜氧供和接触镜配戴: GP – 氧气供应
Notes: 12
12
Corneal O2 Supply with GP Lenses
The supply of O2 to the cornea during GP CL wear is determined by a number of factors.
Most O2 supplied to the cornea diffuses through the lens. Therefore, the O2 permeability of the CL material for an average CL is the prime determinant of O2 supply to the cornea – not the tear exchange under the CL.
Design characteristics such as CL BVP & average thickness play a significant role in determining the O2 transmissibility of the CL in situ. However, GP CLs are routinely applied in a relatively narrow range of centre thicknesses. Given this, the material permeability & BVP are of most significance when considering the O2 performance of a particular GP CL.
O2 is also supplied to the cornea via the tears. The exchange of tear fluid between the tear reservoir at, & under, the CL edge, & the tears in the post-CL tear film, results from CL movement on the eye. This is the so-called ‘tear pump’, the driving force of which is normal blinking.
Despite the much more effective tear pump existing with GP CLs, the tears are a much less effective source of corneal O2 than transmission through highly permeable GP CLs.

## Slide 54
气流通过镜片中的水 (不是聚合体)
含水量范围
聚合体中的水特征
  结合水(不冻水)
  自由水 (冻水)
角膜氧供和接触镜配戴: 软镜渗透率
Notes: 12
12
O2 Permeability of Hydrogel Materials
Typically, polymers used in the production of hydrogel CLs are characterized by their water content. Usually, the water content is expressed as a percentage of the total CL once it is hydrated fully in normal saline.
The temperature should also be stated because the amount of water contained within the CL is temperature dependent. Usually, as a hydrogel’s temperature ↑ its water content ↓ (Tighe, 1989). This has a significant effect on the effective O2 permeability of the material, as will be seen later.

## Slide 55
角膜氧供和接触镜配戴: 含水量– 极化水
CH3
H2C = C
C
CH2
CH2
O
H
O
O
极化水
O
H
H
+
+
–
–
+
O
H
H
+
+
–
O
H
H
+
+
–
羟基 ‘末端’
HEMA 单体
O
H
在羟基末端的极化水
Hydrogen bond
O
H
H
+
+
–
O
H
H
+
+
–
O
H
H
+
+
–
结合水
自由水
–
+

## Slide 56
聚合体-聚合体 吸引
+
–
–
+
H
C
H
H
C
N
H2C
H2C
C = O
CH2
+
N-乙烯基2 吡咯烷酮
吡咯烷酮环
羰基团
O
H
H
+
+
–
O
H
H
+
+
–
极化水
极化水
O
H
CH2
CH2
CH2
CH2
O
H
+
–
–
+
HEMA
HEMA
角膜氧供和接触镜配戴: 含水量– 聚合物因素
Notes: Polymer-polymer attraction (see right hand side of slide).
The presence of other polymer groups, tails, or side-chains competing with water for the same molecular space, or which may shield the charged sites from the water dipole is significant.
The presence of groups, tails or side-chains that may shield charged sites from other large polar species, which, while too big to gain access, allow the water dipole ready access.
O2 flow through a hydrogel CL is dependent on the properties of the water ‘contained’ within the material. O2 passes through the CL by virtue of water’s inherent permeability to such gases. There is no gaseous phase transfer of O2 in hydrogels. All transfer occurs in the dissolved phase, i.e. the movement of O2 through a hydrogel relies on O2’s solubility in water. (Fatt, 1987). O2 molecules do not pass through the material polymer per se, rather they diffuse mostly through the water-filled pores contained within the CL. Some O2 is dissolved in the material itself.
Therefore, the O2 permeability of water is the main limiting factor in the amount of O2 that reaches the cornea via a hydrogel lens. Water is much more permeable to the carbon dioxide leaving the cornea, largely because of its solubility & chemical interaction with water.
To conceptualize dissolved O2, Fatt (1978) uses the analogy of the gas (the identity of the gas is unimportant but it is actually carbon dioxide) present in a sealed aerated (carbonated) beverage. It enters as a gas, is dissolved in the beverage while sealed & exits as a gas once the bottle is opened.
Generally, a material’s O2 permeability ↑ as the water content is ↑. However, the O2 permeability of water itself imposes an upper limit on the amount of O2 that can be delivered to the cornea through a hydrogel CL.
Furthermore, the chemistry of water retention within a hydrogel material also determines how easily O2 can pass through the CL to reach the post-CL tear film. For this reason it is necessary to distinguish between the methods of water retention within the CL matrix.
There are two methods of water retention - bound & free. In a hydrogel material, some of the water, which exists as a charged molecule or dipole, is bound to the polymer electrostatically by the so-called hydrogen bond (see slide). Its properties are changed by this attraction in such a way that it is no longer available as a vehicle for O2 transport through the lens. This bound water is also referred to as non-freezing water (Mirejovsky et al. 1993).
Other factors are involved in water retention at the molecular level. For example, in the case of vinyl pyrrolidone-containing materials, the main water attractant is the negatively charged nitrogen atom in the bulky & relatively rigid pyrrolidone ring (see slide).
Although the ring itself can rotate about its connection to the main polymer backbone (i.e. about the C–N bond) its inflexible properties reduce the attraction between itself & adjacent pyrrolidone rings within the material.
Importantly, the protected nature of N allows water to bond while restricting access by other larger entities.
The charges on the carbonyl group (C=O) are small & contribute little to either polymer-polymer or polymer-water attraction & have only limited significance (this section after Frankland, 1973).
Much of the water within a hydrogel polymer is free to carry O2 from the anterior surface to the cornea. This free water component is also referred to as freezing water. As far as O2 transport is concerned, the ratio of bound to free water is more important than the total water content of the CL material.

## Slide 57
仅自由水可以供氧气通过
结合水和自由水的比例是有影响的
新型聚合物 (含硅)
染色的效果
  不透明染料(影响显著)
  透明染料(很少或没有影响)
角膜氧供和接触镜配戴: 软镜透氧性
Notes: 12
12

## Slide 58
双向阻滞多聚合体
含硅聚合物与水结合
第一代聚合物, 伴随含水量降低透氧性增加 (i.e.较高的含水量是不利因素)
第二代和第三代聚合物透氧性取决于硅分子
角膜氧供和接触镜配戴: 硅水凝胶
广义硅键示意图
R = 另一个原子或分子 例如. 氯 (Cl) 或一个甲基(CH3)
重复链段(单体)
Notes: 12
12
SiHy (silicone hydrogel) materials provide ↑ oxygenation to the cornea & have eliminated hypoxic signs whether worn on a DW or EW basis. The SiHy material permits both O2 & ions to permeate freely through the material by means of two co-continuous phases. It can be described as a biphasic block-copolymer of a highly permeable silicone-based polymer, coupled with a water phase. The transport of O2 molecules occurs via the silicone phase, while ionic & hydraulic permeability takes place through the aqueous phase. A minimum level of ionic & hydraulic permeability is important for CL movement on-eye, especially in low water content materials. 2nd & 3rd generation polymers are intrinsically wettable, which are a combination of monomers & macromers that may (2nd generation) or may not (3rd generation) incorporate an internal wetting agent (polyvinyl pyrrolidone). These later materials do not present the inverse relationship between Dk & water content as per 1st generation polymers. It is important to realize that SiHy materials rely on polymer properties and not water content for their O2 performance, i.e. siloxane materials overcome the limitations placed on O2 performance in hydrogels imparted by their dependence on water content for gas passage. Tellingly, the highest performing SiHy CL material has the LOWEST water content, i.e. a material’s water content is actually a barrier to high O2 performance.

## Slide 59
厚度考虑:
  平均厚度 和中心厚度
  BVP的影响
    正镜, 中心厚度最大, BOZD/FOZD的影响
    负镜, 中心厚度 最小, BOZD/FOZD的影响
影响眼前段的生理反应
角膜氧供和接触镜配戴: 软镜的氧传导性
Notes: 12
12
O2 Transmissibility of Hydrogel Materials
The thickness of a hydrogel CL also influences the amount of O2 transmitted. The thickness characteristics of an SCL influence both the O2 transmissibility & the clinical performance of the lens.
Calculation of SCL O2 transmissibility should take into account the average thickness of the lens. The centre of the CL may not be representative of much of the CL in terms of the amount of O2 delivered to the anterior corneal surface. This is particularly so when considering moderate to high minus powers or plus powered CLs.
Thickness also contributes to the dehydration characteristics of the material both on & off the eye. In general, the thicker the lens, the less it will dehydrate. This is due largely to the greater resistance to the bulk flow of water through the CL offered by thicker lenses.
However, thickness also reduces the O2 transmissibility. If a high water content CL is produced too thin, it causes a higher level of coalescent macro-punctate corneal staining due to pervaporation (Holden et al. 1986), i.e. desiccation or dehydration staining. Therefore, CL designers & prescribers must balance the desire for high transmissibility (thinner lenses) with preventing pervaporation staining (thicker lenses).
O2 transmissibility of a hydrogel CL indicates the expected overall physiological performance of the CL on-eye. Knowing the Dk/t of a CL permits the practitioner to classify it on the basis of the Holden & Mertz criteria for safe daily & overnight wear.

## Slide 60
Dk/t 增加:
  增加含水量（厚度不变）
  减少厚度 (含水量不变)
薄的中等含水量的镜片的 Dk/t最高
严重的镜片沉淀降低Dk/t
角膜氧供和接触镜配戴: 软镜氧传导性
Notes: 12
12
Changes in material water content as well as CL design can affect O2 transmissibility. Based on clinical performance, the practitioner may vary one or both of these variables to achieve higher O2 supply to the cornea.
For practical purposes, the Dk/t of a hydrogel CL is unaffected by mild to moderate deposits on the surface. The O2 transmissibility may be slightly decreased when very heavy deposits accumulate.

## Slide 61
HEMA (38.6%) 材料, 配戴8小时
中心厚度 (mm) 水肿(%)
0.13 8
0.07 5
0.03 1
La Hood, CCLRU Data
软镜日戴
角膜氧供和接触镜配戴: 角膜水肿– 软镜 日戴 HEMA材料
Notes: 12
12
Corneal Swelling with SCL Wear
Among the most commonly used hydrogel polymers is a polymer of hydroxy-ethyl methacrylate (pHEMA), the very first successful soft CL material (Wichtele & Lim, 1950s). HEMA is a low water content (approximately 38.6%), non-ionic material which has been used to fabricate CLs using all existing manufacturing technologies.
Interestingly, the method of manufacture influences the physical properties of the CL that results. O2 permeability is such a factor & one possible reason for the variation in material Dk reported for HEMA is the failure to note the manufacturing technique used to fabricate the test CLs.

## Slide 62
高含水(75%) 材料, 配戴8小时
La Hood, CCLRU Data
软镜日戴
角膜氧供和接触镜配戴: 角膜水肿– 软镜 日戴 高含水
中心厚度 (mm) 水肿(%)
0. 3 2
0.15 0.5
Notes: 12
12
As the thickness of a CL ↑, its O2 transmissibility ↓ & a ↑ corneal swelling results. Over an 8-hour period of wear, an ultra-thin HEMA CL may induce only minimal swelling. A thicker CL such as a toric or a plus power (typical tc = 0.13 mm)  about 8% corneal swelling.
A 0.15 mm thick CL made from a high water content material (e.g. 74%) results in about 0.5% swelling after eight-hours of daily wear. Such CLs are more suitable for toric & plus prescriptions than are lower water content materials. However, the advent of SiHy materials has transformed most aspects of the CL market (sph, toric, high & low BVPs) & are preferred in most cases because of their greater O2 performance.

## Slide 63
配戴8小时
La Hood, CCLRU Data
软镜过夜配戴
角膜氧供和接触镜配戴: 角膜水肿– 软镜长戴
低含水量 12
中含水量 10
高含水量 11
硅水凝胶 4
硅氧烷弹性纤维 2.5
材料 水肿(%)
Notes: 12
12
In myopic hydrogel EW patients, the level of corneal oedema caused during the closed eye phase of wear varies only slightly between CLs that are considered to be optimum for that modality.
Such CLs are:
Ultra thin low water content
Thin mid water content
High water content.
Now, SiHy CLs eclipse most of these considerations.
Typically, hydrogel EW CLs cause about 8-12% corneal swelling following 8 hours of eye closure. This compares very unfavourably with the 3-4% swelling that occurs in the average non-CL wearing eye.
Recent developments in SiHy materials for SCL EW have produced a significantly ↓ swelling response of approximately 2–3% after 8 hours of sleep. In a study by Fonn et al. (1998) comparing high Dk (140) siloxane-containing hydrogel CLs (lotrafilcon A) with low Dk (28) hydrogel CLs (etafilcon A), overnight corneal swelling after 8 hours sleep was 2.7% (SD ±0.4%) with the high Dk CLs & 8.6% (SD ±0.6%) with the low Dk lenses. The new generation CLs delivering much higher transmissibilities than previously are being used to re-launch soft CL EW.

## Slide 64
配戴8小时
La Hood, CCLRU Data
GP 日戴
角膜氧供和接触镜配戴: 角膜水肿– GP 日戴
材料 水肿 (%)
PMMA 6
低Dk 3 - 4
中Dk 1
高Dk 0
Notes: 12
12
Corneal Swelling with GP CL Wear
The higher level of O2 transmissibility achievable with GP CLs compared with SCLs results in less corneal swelling during DW. The additional supply of O2 via the tear pumping mechanism with GP lenses, also contributes to the low levels of oedema. Only very low Dk/t GP CLs cause any significant corneal swelling. Consequently, there is little reason to continue to use such CL materials
When GP CLs of low O2 transmissibility are worn overnight, the level of corneal oedema induced is very similar to the best results achievable with current conventional hydrogel lenses.

## Slide 65
8小时配戴
La Hood, CCLRU Data
GP 过夜配戴
角膜氧供和接触镜配戴: 角膜水肿 – GP 长戴
材料 水肿 (%)
低 Dk 10 - 13
中 Dk 7 - 9
高 Dk 5 - 6
Notes: 12
12
When highly O2 transmissible GP CLs are worn overnight, the 5-6% corneal swelling that occurs compares favourably with the 3-4% in a non-wearer. In EW, a major advantage of GP CLs over SCLs is the rapidity with which the induced corneal oedema resolves following eye opening. This is due primarily to the superior O2 transmissibility of GP lenses (cf. hydrogel SCLs), as well as the tear exchange that occurs when the CLs begin to move on the cornea once blinking is re-established. Incomplete corneal coverage is also helpful.

## Slide 66
评估最低透氧，避免引起与接触镜的相关眼部生理改变
标准 | Dk/t | 来源
角膜中心无水肿 | 20 - 24 | 人
角膜周边无水肿 | 33 | 人
类似无镜片的角膜缘充血 | 125 | 人
镜片下方氧气张力是大气中的75% | 140 | 人
避免上皮酸中毒 | 300 | 兔子
避免房水酸中毒 | 18 | 兔子
角膜氧供和接触镜配戴:最低氧传导性– 睁眼时

## Slide 67
数字模型评估最低透氧，避免引起与接触镜有关的生理变化
Criteria | Dk/t | Source
避免中央基质缺氧 | 20 | 模型
避免周边基质缺氧 | 100 | 模型
中央氧剖面类似于无镜片 | 100 | 模型
周边氧剖面类似于无镜片 | >200 | 模型
完全氧化 | 40 | 模型
避免中央基质缺氧 | 20 | 模型
角膜氧供和接触镜配戴: 最小氧传导性– 睁眼时
Notes: See last slide of this lecture for further references.

## Slide 68
评估最小Dk/t 值，避免引起与接触镜有关的生理变化
标准 | Dk/t | 来源
过夜配戴后角膜中央水肿4% | 75 - 87 | 人
乳酸脱氢酶 (LDH) 活性 | 84 | 兔子
角膜氧供和接触镜配戴: 最小氧传导性– 闭眼时
Notes: See last slide of this lecture for further references.

## Slide 69
数字模型评估最小DK/T值，避免引起与接触镜的相关眼部生理改变
标准 | Dk/t | 来源
避免中央基质层缺氧 | 200 | 模型
5% 角膜细胞缺氧 | 90 | 模型
5% 角膜细胞乳酸升高 | 200 | 模型
完全氧化 | 100 - 120 | 模型
角膜氧供和接触镜配戴: 最小氧传导性– 闭眼时
Notes: See last slide of this lecture for further references.

## Slide 70
降低有氧糖代谢
乳酸积累（基质）
基质酸化
渗透压失调
水肿
结构改变
角膜氧供和接触镜配戴: 角膜缺氧的生理影响
Notes: 12
12
Effects of Corneal Hypoxia
Any ↓ in the supply of O2 to the cornea can have significant effects on normal metabolic activity. The effects are numerous & they range from mild to severe in their impact on the cornea.
Assessment of the effects of hypoxia on the eye provides a better understanding of corneal O2 requirements. A number of in vivo studies have attempted to define the level of O2 required by the cornea to prevent the occurrence of changes in structure or function.

## Slide 71
角膜表面氧分压是多少时才能防止角膜的不良变化？
角膜氧供和接触镜配戴: 氧供& 角膜改变
Notes: 12
12
O2 Tension & Corneal Changes
A large number of studies have examined the effect of changes to the pre-corneal O2 tension & any resultant oedema of the corneal tissue.
Other effects from reduced O2 supply to the cornea include changes to the:
Epithelial mitotic rate
Density of nerve fibre endings.
Sensitivity of the cornea
Corneal pH.

## Slide 72
需要9% O2 以预防:
  有丝分裂的减缓
  前房乳酸的堆积
角膜氧供和接触镜配戴: 上皮有丝分裂
Notes: 12
12
O2 Supply & Epithelial Mitosis
Hamano (1985) showed that when the O2 level falls below 9%, a significant ↓ in rabbit epithelial mitotic configurations occurs compared with that in the control eyes.
Glucose metabolism within the cornea is related to the amount of O2 available to the tissue. It can be quantified in terms of the accumulation of lactate in the anterior chamber, which ↑ as the O2 supply ↓. To prevent the build-up of lactate, Hamano (1985) suggested that the level of O2 must be 9% or higher.

## Slide 73
动物实验
缺氧降低角膜神经末梢密度
需要9 - 10% 氧气
角膜氧供和接触镜配戴: 角膜神经纤维末梢
Notes: 12
12
Corneal Nerve Fibre Endings
Hamano (1985) also examined the effects of CL EW on the nerve fibre terminal endings in the rabbit.
Hypoxia caused the density of the terminal endings to ↓. His study determined that the O2 level required to maintain the nerve fibres in their normal state is 9–10%.

## Slide 74
角膜触觉域值增加 (敏感度降低) :
  过长时间闭眼
  接触镜配戴
  缺氧
需要8% 氧气保持角膜触觉阈值
角膜氧供和接触镜配戴: 角膜敏感度
Notes: 12
12
Corneal Sensitivity & CL Wear
The cornea is the most densely innervated tissue in the body. This innervation protects the eye by making it highly sensitive & responsive to foreign bodies, abrasion, etc.
Millodot (e.g. 1984) has demonstrated that the cornea can be affected by a number of conditions to a point where the ability of the cornea to perceive a stimulus is severely reduced. He examined the touch threshold of the cornea using a Cochet-Bonnet aesthesiometer & found that hypoxia of the cornea resulted in an ↑ in the touch threshold value. Such an effect could make the cornea more susceptible to serious damage as the normal defensive mechanisms & reactions are absent or reduced.
A minimum of 8% O2 is required to maintain corneal sensitivity at or near a normal level for the average person (Millodot & O’Leary, 1980).

## Slide 75
荧光测定法进行测定
pH值降低
  闭眼
  缺氧
  接触镜配戴
空泡反应
保持正常PH值:
  上皮: 需要21% 氧分压
  内皮/房水: 需要8%氧分压
角膜氧供和接触镜配戴: 角膜PH值
Notes: 12
12
Corneal pH & CL Wear
Bonanno & Polse (1987b) demonstrated that the corneal stromal environment becomes more acidic (↓ pH) in a range of circumstances including CL wear.
It is postulated that a reduction (Holden et al., 1985) or changes (Williams, 1986) in corneal pH cause the endothelial bleb response.
It has been estimated that in the rabbit, a Dk/t of greater than 300 (x10–9) is required to prevent epithelial intracellular pH changes in the open eye (Giasson & Bonanno, 1994). This suggests an EOP of about 21% (calculation using the equation from Holden & Mertz, 1984, shows 25.5%, an impossibility under normal atmospheric circumstances, i.e. supranormal O2 levels). This implies unhindered access to atmospheric O2. By way of contrast, a Dk/t of only 18 (x10–9 ) is required to prevent aqueous pH changes (Giasson & Bonanno, 1994). This suggests an EOP of only about 8% is required.

## Slide 76
降低氧气供应 (依赖于睑结膜)
部分眼睑闭合效应?
降低泪液渗透压
增加二氧化碳分压
降低泪液和基质PH值
增加角膜温度 (至 37oC)
角膜氧供和接触镜配戴: 闭眼时
Notes: 12
12
Effects of Eye Closure
When the eyelids are open, the majority of O2 supplied to the cornea comes from the atmosphere.
During sleep, the lids are closed & significant changes take place in the ocular environment.
The main change is a ↓ in the O2 supply to the cornea. When the lids are closed the major source of supply becomes the palpebral conjunctival vessels. Some atmospheric O2 may reach the cornea if the lids are only partially closed (lagophthalmos) & some may be supplied by the bulbar conjunctival vessels.
For the latter to be effective, some tear movement would be required. Rapid eye movement (REM) sleep could provide such movement but it is likely to result in only limited tear exchange.
Lid closure also causes a build-up in the levels of CO2 in the cornea & results in an acidic pH shift in the tear film & stroma. The tear osmolality also ↓ during sleep.

## Slide 77
氧分压大约55 mm Hg
不配戴接触镜，8小时后角膜水肿大约3.5%
睁眼后快速消肿
改变代谢活动?
降低氧气需求?
角膜氧供和接触镜配戴: 闭眼时
Notes: 12
12
Corneal Swelling with Eye Closure
Following eye closure, the anterior corneal O2 tension falls rapidly to a steady state level of about 55 mm Hg (for further details see earlier in this lecture). This hypoxic state causes the cornea to swell.
The literature suggest that the average amount of overnight swelling, i.e. swelling that occurs following 8 hours of eye closure when no CL is worn, is between 3 an 5.5% (e.g. 3%: Sweeney, 1991, 5.5%: Harper et al., 1996, most other studies fall between these limits).
When the eyelids are opened following sleep, the corneal oedema resolves quickly & the corneal thickness returns to normal.
Closed Eye
It is possible that, during periods of closed-eye sleep, there is a physiological reduction in metabolic activity that offsets the ↓ availability of O2. If this is the case, the cells would presumably have a lower requirement for O2 & could function effectively with less O2.

## Slide 78
上皮和基质水肿
  透明度降低
微囊和空泡
条纹
褶皱
内皮空泡
内皮细胞多形化
新生血管
裂隙灯观察- 角膜
角膜氧供和接触镜配戴: 缺氧导致结构改变
Notes: 12
12
Hypoxia & Structural Changes to the Cornea
Both short-term & chronic corneal hypoxia can result in significant changes in the structure & function of corneal tissue. In most cases, even subtle changes are visible with the slit-lamp biomicroscope.
All layers of the cornea can be affected by hypoxia. The CL practitioner must look for signs of hypoxia at each after-care examination (see Lectures 4.4 & 4.5 & Module 7 of the original ICLC).

## Slide 79
CRITERION
角膜水肿
上皮细胞有丝分裂
上皮愈合
角膜敏感度
糖元消耗
内皮空泡
神经末梢密度
自然概念
MINIMUM O2 (%)
日戴: 9.9%, 长戴: 17.9%
13.2%
10.4%
7.7%
5%
15 - 16.6%
9 - 10%
20.946% ±0.002%
角膜氧供和接触镜配戴: 最小需氧量
Notes: O2 Requirements: Summary
The minimum O2 level preferred by the eye is probably 20.95%, i.e. the level of O2 generally available at sea level.
However, many people live the whole of their lives in environments in which less O2 than this is available because of the altitude at which they live. Further, for about one-third of our lives, the anterior eye is exposed to only about one-third of this level of O2 during eye closure & sleep.
Therefore, it may be more appropriate to think in terms of a desired minimum rather than an absolute minimum, despite the results of numerous studies offering minima based on study outcomes & the individual variation demonstrated. Such results are limited by study design, stimulus limitations, non-human subjects and, frequently, the lack of reality of the environment applied.
Rather than a ‘minimum’ level perhaps we should be using the term ‘optimum’, ‘ideal’, ‘recommended’ or as some authors use, ‘critical’ minimum level. Fatt used the phrase ‘critical O2 requirement’ or COR.
Recommendations from some studies cannot be applied too rigorously since they exceed the levels available in many high-altitude regions of the world. The inhabitants of such regions thrive despite their ‘O2 deprivation’.

## Slide 80
角膜氧供和接触镜配戴: 最小需氧量
睁眼
代谢模型
镜片滑落
镜片氧传导性

## Slide 81
Papas EB, 2014. The significance of oxygen during contact lens wear. CL Ant Eye. 37(6): 394 - 404. doi: 10.1016/j.clae.2014.07.012. Epub 2014 Aug 16 . . Takatori SC et al., 2012. In vivo oxygen uptake into the human cornea. Invest Ophthalmol Vis Sci. 53(10): 6331 – 6337.
Takatori SC et al., 2013. In vivo oxygen uptake during soft-contact-lens wear. Invest Ophthalmol Vis Sci.. 54(5): 3472 - 3479. doi: 10.1167/iovs.12-11169.
Percy Lazon De La Jara et al., 2013 (May). Corneal Uptake of Oxygen In Vivo During Soft Contact Lens Wear (ARVO Abstract) Conclusions: Application of the classical procedure to our experimental data gives corneal-uptake results that are about three to five times smaller those reported classically. According to our corrected procedure, full oxygenation of the human eye, 11.3 μL/cm2 /h for the 10 subjects studied, is reached only asymptotically (see Fig. 1). That is, very high lens transmissibility is required before the lens no longer impedes oxygen transport. Conversely, 95 % anterior corneal oxygenation is achieved with a lens transmissibility of 150 hBarrer/cm.
O2 & CLs: Minimum O2 – Further Reading

## Slide 82: Please visit us online at:
www.iacle.org